Technical data for enquiry (remover of sulfur compounds and water for FA-907 A/B, Charge Solid KOH Tower

# Requirements

- The material should be suitable for removing sulfur compounds and water from benzene.

- Required quantity: 5 000 kg for reactor.

- Required material type: main component - potassium hydroxide, content in (%): ≥ 89.5 %.

- Material characteristics: solid substance in the form of pellets (briquettes).

- The material must be able to remove the content of sulfur compounds below 1 ppm (wt.) and the water content below 200 ppm (wt.) throughout its lifetime. Product quality must be guaranteed.

- The service life of the material must not be shorter than 3 years. Lifetime should be guaranteed.

- The properties of the material and its lifetime should be guaranteed. If the limit of 1 ppm (wt.) of sulfur and 200 ppm (wt.) of water is exceeded before the end of the guaranteed time, the supplier must be obliged to replace the material with fresh material or return the costs in proportion to the remaining guaranteed time.

- Delivery time: until March 2025.

- Minimum shelf life: 4 months.

# The offer should contain the following information:

- Material type and chemical composition.

- Diameter [mm] and shape of material particle.

- Bulk density [kg/m3].

- Minimum guaranteed lifetime.

- Terms of guarantee.

- Packing type (barrel).

# Operating Conditions

| ADSORPTION |  |  |
| --- | --- | --- |
| Feed phase |  | Liquid |
| Flow Direction |  | Up |
| Feed Flow Rate, kg/h | normal | 18 000 |
|  | max | 28 000 |
| Temperature °C | normal | 35 |
|  | max | 64 |
| Pressure (g), bar | normal | 2.0 |
|  | max | 7.9 |
| Molecular Weight, g/mol |  | 78.12 |
| Density, kg/m3 |  | 856.5 |
| Feed Composition, % hm. | benzene | 99.9 |
|  | toluene | 0.1 |

# Adsorbers dimensions and configuration (Vessel Details)

- There are 2 identical vessels FA-907A and FA-907B

- Mode of operation: one absorber in operation, the other in reserve

- Insulation					External

- Internal Diameter, mm				1 900

- Height (filling), mm		             	3 050

- Actual Material Life time, years                          5